Supporting Information

for

Cobalt Single-Atom Oxidase Mimics for Glucose Oxidase-Free Cascade Colorimetric Detection of α-Glucosidase Activity

Chuanxia Chen a,b,*, Taoming Xu a, Xiaohui Gong a, Zongyu Han a, Yawen Liu a, Feifan Zhang a, Guoping Wang b,*, Yizhong Lu a,*

aSchool of Materials Science and Engineering, University of Jinan, Jinan 250022, China

bZhejiang Dayang Biotechnology Group Co., Ltd, Hangzhou, Zhejiang311616, China

*Corresponding authors: mse_chencx@ujn.edu.cn (C. Chen); yuiop380@sina.com (G. Wang); mse_luyz@ujn.edu.cn (Y. Lu)

Figure S1 TEM image of Co-NC.

Figure S2 TEM images of (a-b) ZIF-8 and (c-d) Co@ ZIF-8.

Figure S3 TEM images of NC.

Figure S4 Effect of (a) pH and (b) temperature on the Co-NC catalyzed oxidation of TMB.

Figure S5 Time-dependent absorbance changes of the reaction solutions at different Co-NC concentrations.

Figure S6 UV-Vis absorption spectra of the TMB oxidation systems in the absence of catalyst (Control), and in the presence of pristine NC or Co-NC nanozyme.

Figure S7 Verification of the non-H2O2 generation pathway during the Co-NC catalytic process. (a) Photographic illustration of the verification experiment. (b) The corresponding UV-Vis absorption spectra. The absence of the characteristic blue product (grey line) confirms that no free H2O2 was generated in the Co-NC-catalyzed oxidation system. The subsequent addition of external H2O2 triggered a distinct colorimetric response (blue line), serving as a positive control.

Figure S8 Lineweaver-Burk double reciprocal plot for the Co-NC-catalyzed oxidation of TMB.

Table S1 Kinetic parameters of the Co-NC and other Co-based catalysts

| Sample | Km (mM) | Vmax (M·s-1) | Ref. |
| --- | --- | --- | --- |
| CoRu/G Co3O4 nanoparticles | 0.015 0.051 | 21.5×10−8 3.30×10−8 | [1] [2] |
| MnCo2O4 | 0.009 | 6.04×10−8 | [3] |
| Natural HPR/H2O2 | 0.434 | 10.0×10-8 | [4] |
| Co(OH)2 nanocages | 0.362 | 6.06×10-8 | [5] |
| Co nanoparticles/H2O2 | 5.09 | 9.98×10−8 | [6] |
| NiCo2O4/H2O2 | 0.142 | 2.22×10−8 | [7] |
| CoNPs/MC/H2O2 | 0.39 | 13.4×10−8 | [8] |
| Co/C nanohybrid | 0.071 | 23.2×10-8 | [9] |
| C-CoCu-HNC | 0.0741 | 2.56 × 10−8 | [10] |
| Co-NC | 0.234 | 9.83× 10−8 | This work |

Table S2 Comparison of various HQ assays

| Method | Mode | Materials | Detection range (μM) | LOD (μM) | Ref |
| --- | --- | --- | --- | --- | --- |
| Electrochemical | Turn-on | Au-Pd nanoflower/rGO | 1.6-100 | 0.5 | [11] |
| Fluorometry | Turn-off | CdTe QDs | 0.5-500 | 0.5 | [12] |
| Colorimetry | Turn-off | FeCo@C | 0–30 | 0.8 | [13] |
| Colorimetry | Turn-off | MnO2@CuAl-CLDHs | 1–100 | 0.183 | [14] |
| Colorimetry | Turn-off | CoFe LDH/H2O2 | 0–500 | 2.2 | [15] |
| Colorimetry | Turn-off | Fe-CDs/H2O2 | 2–15 | 0.282 | [16] |
| Colorimetry | Turn-off | SA-Pt/CN | 1–10 | 0.07 | [17] |
| Colorimetry | Turn-on | Co-NC | 0–100,100–400 | 0.26 | This work |

Figure S9 The absorbance at 507 nm recorded in the presence of HQ, phenol, and various interfering inorganic ions.

Figure S10 Effect of the enzymatic hydrolysis time on the absorbance of the cascade sensing system.

Figure S11 Effect of the enzymatic a-Arbutin concentration on the absorbance of the cascade sensing system.

Table S3 Comparison of various methods for the determination of α-Glu

| Materials | Method | Detection range (U/mL) | LOD (mU/mL) | Ref |
| --- | --- | --- | --- | --- |
| pAPG-AuNPs | Electrochemical | 0.01–1.3 | 5 | [18] |
| b-CDs | Fluorometry | 0.13–6.7 | 36 | [19] |
| Si QDs-MnO2 | Fluorometry | 0.02–2.5 | 7 | [20] |
| Magnetic nanospheres | Fluorometry | 0.4–1.7 | 23 | [21] |
| AgInZnS QDs | Fluorometry | 0.01–0.16 | 7.3 | [22] |
| MnO2 NS/OPD/AuNCs | Fluorometry | 0.2–8 | 30 | [23] |
| β-CD-CQDs | Fluorometry | 0.01–0.06 | 0.6 | [24] |
| CDs | Fluorometry | 0.2–10 | 10 | [25] |
| PBA-CQD | Fluorometry | 1.14–17.35 | 0.33 | [26] |
| F-PDA-CoOOH | Fluorometry | 0.002–0.08 | 1.65 | [27] |
| Fe NZs+NCDs | Fluorometry | 0.005–0.1 | 2.4 | [28] |
| AuNCs | Dual-channel | Colorimetry:0.25–0.95 Fluorometry: 0.25–0.95 | 21 12 | [29] |
| Si CNPs | Dual-channel | Colorimetry: 0.006–3 Fluorometry: 0.006–2.1 | 4.6 3.2 | [30] |
| Tb-CuGMP NPs | Dual-channel | Colorimetry: 0.004–0.03 Fluorometry: 0.002–0.1 | 2.1 0.51 | [31] |
| AuNPs-I--Cys-GOx | Colorimetry | 0.0025–0.05 | 1 | [32] |
| Cu-N-C | Colorimetry | 0.00025 to 0.008 | 0.09 | [33] |
| SA-Pt/CN | Colorimetry | 0.01–8 | 3.8 | [17] |
| pAPG-AuNPs | Colorimetry | 0.01–1.1 | 4 | [34] |
| f-FeNC | Colorimetry | 0.005–0.04, 0.04–0.1 | 0.27 | [35] |
| Co-NC | Colorimetry | 0.001–0.08, 0.08–0.3 | 0.19 | This work |

Table S4 Determination of α-Glu activity in real samples

| Sample | Added (mU/mL) | Found (mU/mL) | Recovery (%) | RSD (n = 3, %) |
| --- | --- | --- | --- | --- |
| Serum 1 | 0 | − | − | 1.3 |
|  | 30 | 30.34 | 101.1 | 4.2 |
|  | 60 | 58.24 | 97.1 | 3.5 |
| Serum 2 | 0 | − | − | 2.1 |
|  | 30 | 31.42 | 104.7 | 5.6 |
|  | 60 | 61.73 | 102.9 | 4.4 |

Reference

- Keoingthong, P.; Li, S.; Zhu, Z.; et al. Enzyme-Mimic Activity Study of Superstable and Ultrasmall Graphene Encapsuled CoRu Nanocrystal. APL Mater. 2021, 9, 051110. https://doi.org/10.1063/5.0048777.

- Qin, W.; Su, L.; Yang, C.; et al. Colorimetric Detection of Sulfite in Foods by a TMB–O2–Co3O4 Nanoparticles Detection System. J. Agric. Food Chem. 2014, 62, 5827–5834. https://doi.org/10.1021/jf500950p.

- Huang, L.; Chen, K.; Zhang, W.; et al. ssDNA-Tailorable Oxidase-Mimicking Activity of Spinel MnCo2O4 for Sensitive Biomolecular Detection in Food Sample. Sens. Actuators B Chem 2018, 269, 79–87. https://doi.org/10.1016/j.snb.2018.04.150.

- Gao, L.; Zhuang, J.; Nie, L.; et al. Intrinsic Peroxidase-like Activity of Ferromagnetic Nanoparticles. Nat. Nanotechnol. 2007, 2, 577–583. https://doi.org/10.1038/nnano.2007.260.

- Zhu, H.; Quan, Z.; Hou, H.; et al. A Colorimetric Immunoassay Based on Cobalt Hydroxide Nanocages as Oxidase Mimics for Detection of Ochratoxin A. Anal. Chim. Acta 2020, 1132, 101–109. https://doi.org/10.1016/j.aca.2020.07.068.

- Chen, Y.; Cao, H.; Shi, W.; et al. Fe–Co Bimetallic Alloy Nanoparticles as a Highly Active Peroxidase Mimetic and Its Application in Biosensing. Chem. Commun. 2013, 49, 5013–5015. https://doi.org/10.1039/c3cc41569d.

- Su, L.; Dong, W.; Wu, C.; et al. The Peroxidase and Oxidase-like Activity of NiCo2O4 Mesoporous Spheres: Mechanistic Understanding and Colorimetric Biosensing. Anal. Chim. Acta 2017, 951, 124–132. https://doi.org/10.1016/j.aca.2016.11.035.

- Dong, W.; Zhuang, Y.; Li, S.; et al. High Peroxidase-like Activity of Metallic Cobalt Nanoparticles Encapsulated in Metal–Organic Frameworks Derived Carbon for Biosensing. Sens. Actuators B Chem. 2018, 255, 2050–2057. https://doi.org/10.1016/j.snb.2017.09.013.

- Chen, J.; Zheng, X.; Zhang, J.; et al. Bubble-Templated Synthesis of Nanocatalyst Co/C as NADH Oxidase Mimic. Natl. Sci. Rev. 2022, 9, nwab186. https://doi.org/10.1093/nsr/nwab186.

- Li, S.; Hou, Y.; Chen, Q.; et al. Promoting Active Sites in MOF-Derived Homobimetallic Hollow Nanocages as a High-Performance Multifunctional Nanozyme Catalyst for Biosensing and Organic Pollutant Degradation. ACS Appl. Mater. Interfaces 2020, 12, 2581–2590. https://doi.org/10.1021/acsami.9b20275.

- Chen, Y.; Liu, X.; Zhang, S.; et al. Ultrasensitive and Simultaneous Detection of Hydroquinone, Catechol and Resorcinol Based on the Electrochemical Co-Reduction Prepared Au-Pd Nanoflower/Reduced Graphene Oxide Nanocomposite. Electrochim. Acta 2017, 231, 677–685. https://doi.org/10.1016/j.electacta.2017.02.060.

- Yuan, J.; Guo, W.; Wang, E. Utilizing a CdTe Quantum Dots−Enzyme Hybrid System for the Determination of Both Phenolic Compounds and Hydrogen Peroxide. Anal. Chem. 2008, 80, 1141–1145. https://doi.org/10.1021/ac0713048.

- Wu, T.; Ma, Z.; Li, P.; et al. Bifunctional Colorimetric Biosensors via Regulation of the Dual Nanoenzyme Activity of Carbonized FeCo-ZIF. Sens. Actuators B Chem. 2019, 290, 357–363. https://doi.org/10.1016/j.snb.2019.03.130.

- Xing, N.; Yang, L.; Wang, L.; et al. Cu/Mn Synergy Catalysis-Based Colorimetric Sensor for Visual Detection of Hydroquinone. Coatings 2024, 14, 453. https://doi.org/10.3390/coatings14040453.

- Wang, Z.; Ren, Q.; Han, L.; et al. Synergistic Electronic Modulation in Cysteine-Functionalized CoFeMn-LDH Heterophase Nanozymes: Multi-Interface Engineering for Smartphone-Enabled Ultrasensitive Hydroquinone Sensing. Chem. Eng. J. 2025, 520, 165749. https://doi.org/10.1016/j.cej.2025.165749.

- Song, H.; Liu, F.; Wang, T.; et al. Peroxidase-like Activity of Iron-Doped Carbon Dots with Efficient 1O2 Production for Colorimetric and Photothermal Dual-Mode Detection of α-Glucosidase and Its Inhibitors. Microchem. J. 2025, 216, 114830. https://doi.org/10.1016/j.microc.2025.114830.

- Kang, G.; Liu, W.; Liu, F.; et al. Single-Atom Pt Catalysts as Oxidase Mimic for P-Benzoquinone and α-Glucosidase Activity Detection. Chem. Eng. J. 2022, 449, 137855. https://doi.org/10.1016/j.cej.2022.137855.

- Li, J.; He, G.; Wang, B.; et al. Fabrication of Reusable Electrochemical Biosensor and Its Application for the Assay of α-Glucosidase Activity. Anal. Chim. Acta 2018, 1026, 140–146. https://doi.org/10.1016/j.aca.2018.04.015.

- Cheng, X.; Xu, J.; Wang, L.; et al. A Redox Modulated Ratiometric Fluorometric Method Based on the Use of Dual-Color Carbon Dots for Determination of the Activity of Enzymes Participating in Ascorbic Acid-Related Reactions. Microchim. Acta 2019, 186, 818. https://doi.org/10.1007/s00604-019-3820-z.

- Liu, J.; Duan, X.; Wang, M.; et al. A Label-Free Fluorescent Sensor Based on Silicon Quantum Dots–MnO2 Nanosheets for the Detection of α-Glucosidase and Its Inhibitor. Anal. 2019, 144, 7398–7405. https://doi.org/10.1039/c9an01680e.

- Yue, X.; Su, L.; Chen, X.; et al. A New Method for the in Situ Assay of α-Glucosidase Activity and Inhibitor Screening through an Enzyme Substrate-Mediated DNA Hybridization Chain Reaction. New J. Chem. 2019, 43, 9458–9465. https://doi.org/10.1039/c9nj01868a.

- Zhang, J.; Liu, J.; Wang, M.; et al. A Fluorometric Assay for α-Glucosidase Activity Based on Quaternary AgInZnS QDs. Microchim. Acta 2021, 188, 227. https://doi.org/10.1007/s00604-021-04855-5.

- Shi, M.; Cen, Y.; Xu, G.; et al. Ratiometric Fluorescence Monitoring of α-Glucosidase Activity Based on Oxidase-like Property of MnO2 Nanosheet and Its Application for Inhibitor Screening. Anal. Chim. Acta 2019, 1077, 225–231. https://doi.org/10.1016/j.aca.2019.05.037.

- Tang, C.; Qian, Z.; Qian, Y.; et al. A Fluorometric and Real-Time Assay for α-Glucosidase Activity through Supramolecular Self-Assembly and Its Application for Inhibitor Screening. Sens. Actuators B Chem 2017, 245, 282–289. https://doi.org/10.1016/j.snb.2017.01.150.

- Kong, W.; Wu, D.; Xia, L.; et al. Carbon Dots for Fluorescent Detection of α-Glucosidase Activity Using Enzyme Activated Inner Filter Effect and Its Application to Anti-Diabetic Drug Discovery. Anal. Chim. Acta 2017, 973, 91–99. https://doi.org/10.1016/j.aca.2017.03.050.

- Ao, H.; Feng, H.; Huang, X.; et al. A Reversible Fluorescence Nanoswitch Based on Dynamic Covalent B–O Bonds Using Functional Carbon Quantum Dots and Its Application for α-Glucosidase Activity Monitoring. J. Mater. Chem. C 2017, 5, 2826–2832. https://doi.org/10.1039/c7tc00223h.

- Zhang, H.; Wang, Z.; Yang, X.; et al. The Determination of α-Glucosidase Activity through a Nano Fluorescent Sensor of F-PDA−CoOOH. Anal. Chim. Acta 2019, 1080, 170–177. https://doi.org/10.1016/j.aca.2019.07.014.

- Lv, Y.; Zhou, C.; Li, M.; et al. A Dual-Mode Sensing System Based on Carbon Quantum Dots and Fe Nanozymes for the Detection of α-Glucosidase and Its Inhibitors. Talanta 2024, 268, 125328. https://doi.org/10.1016/j.talanta.2023.125328.

- Li, S.; Zhang, H.; Huang, Z.; et al. Fluorometric and Colorimetric Dual-Mode Sensing of α-Glucosidase Based on Aggregation-Induced Emission Enhancement of AuNCs. J. Mater. Chem. B 2024, 12, 1550–1557. https://doi.org/10.1039/d3tb02532b.

- Nsanzamahoro, S.; Wang, W.F.; Zhang, Y.; et al. Alpha-Glucosidase-Triggered Reaction for Fluorometric and Colorimetric Assays Based on the Formation of Silicon-Containing Nanoparticles. Anal. Chem. 2021, 93, 15412–15419. https://doi.org/10.1021/acs.analchem.1c03210.

- Bezuneh, T.T.; Nan, F.; Li, X.; et al. Self-Cascading Nucleotide-Based Nanozyme for Ultra-Sensitive Dual-Signal Detection of α-Glucosidase Activity. Talanta 2026, 297, 128726. https://doi.org/10.1016/j.talanta.2025.128726.

- Chen, H.; Zhang, J.; Wu, H.; et al. Sensitive Colorimetric Assays for α-Glucosidase Activity and Inhibitor Screening Based on Unmodified Gold Nanoparticles. Anal. Chim. Acta 2015, 875, 92–98. https://doi.org/10.1016/j.aca.2015.02.022.

- Jiang, Y.; Chen, Z.; Yuan, Y.; et al. Cu–N–C Single-Atom Nanozyme as an Ultrasensitive Sensing Platform for α-Glucosidase Detection. Mater. Today Chem. 2024, 41, 102327. https://doi.org/10.1016/j.mtchem.2024.102327.

- Zhang, J.; Liu, Y.; Lv, J.; et al. A Colorimetric Method for α-Glucosidase Activity Assay and Its Inhibitor Screening Based on Aggregation of Gold Nanoparticles Induced by Specific Recognition between Phenylenediboronic Acid and 4-Aminophenyl-α-D-Glucopyranoside. Nano Res. 2014, 8, 920–930. https://doi.org/10.1007/s12274-014-0573-1.

- Zhang, C.; Chen, C.; Zhao, D.; et al. Multienzyme Cascades Based on Highly Efficient Metal-Nitrogen- Carbon Nanozymes for Construction of Versatile Bioassays. Anal. Chem. 2022, 94, 3485–3493. https://doi.org/10.1021/acs.analchem.1c04018.