Sustained Lithium Nitrate Release in Gel Polymer Electrolytes Enabled by Bulk Reservoir

Xinyue Zhaoa†, Yu Zhaob†, Kanghou Maa, Jingyi Hana, Ningning Wuc*, Yaohui Zhanga*

a School of Physics, Harbin Institute of Technology, Harbin, Heilongjiang, 150001, China

b School of Chemistry, Harbin Institute of Technology, Harbin, Heilongjiang, 150001, China

c School of Electrical Engineering, Hebei University of Technology, Tianjin, 300401, China

†These authors contributed equally to this work and share first authorship

*Corresponding authors. E-mail address: hitcrazyzyh@hit.edu.cn, 2024042@hebut.edu.cn

Supplementary Figures

As shown in Figures S1 and S2, C-LiNO3-10% GPE exhibits the best cycling performance among the samples with different LiNO3 loadings. A lower loading provides insufficient interfacial regulation, whereas excessive LiNO3 release may compromise membrane uniformity and ion transport; therefore, 10% was selected as the optimized loading for subsequent studies.

Figure S1. Cycling performance and Coulombic efficiency of LFP full cells using S-LiNO3 and C-LiNO3 GPEs with different LiNO3 contents at 1 C.

Figure S2. NO3− concentration changes in ester-based electrolyte after repeated soaking (6 h each) for C-LiNO3-5%, C-LiNO3-10% and C-LiNO3-15% GPE.

Figure S3. Cross-sectional EDS mapping of a) S-LiNO3 and b) C-LiNO3 GPEs.

Figure S4. DSC comparison of Bare GPE, S-LiNO3 GPE, and C-LiNO3 GPE.

Table S1. The calculation results of the crystallinity of GPEs in DSC.

| GPE | Crystallinity (%) |
| --- | --- |
|  | DSC |
| Bare GPE | 52.48 |
| S-LiNO3 GPE | 48.91 |
| C-LiNO3 GPE | 43.55 |

Figure S5. Tensile stress-strain curves of Bare GPE, S-LiNO3 GPE, and C-LiNO3 GPE.

Figure S6. Corresponding Arrhenius plots of the Bare, S-LiNO3, and C-LiNO3 GPEs.

Table S2. Temperature-dependent ionic conductivities of the Bare, S-LiNO3, and C-LiNO3 GPEs.

| Temperature (℃) | 1000/T (K⁻1) | Bare | S-LiNO3 | C-LiNO3 |
| --- | --- | --- | --- | --- |
| 30 | 3.2987 | 0.829 | 0.914 | 1.110 |
| 40 | 3.1934 | 0.970 | 1.080 | 1.340 |
| 50 | 3.0945 | 1.110 | 1.290 | 1.490 |
| 60 | 3.0017 | 1.180 | 1.430 | 1.640 |
| 70 | 2.9142 | 1.280 | 1.630 | 1.800 |

Table S3. Ionic conductivity at 30°C, Li⁺ transference number, apparent activation energy, and fitting coefficient of different GPEs.

| GPE | σ30℃ (10−3 S cm⁻1) | TLi+ | Ea (kJ mol⁻1) | R2 |
| --- | --- | --- | --- | --- |
| Bare | 0.829 | 0.31 | 9.56 | 0.9765 |
| S-LiNO3 | 0.914 | 0.56 | 12.46 | 0.9950 |
| C-LiNO3 | 1.110 | 0.62 | 10.06 | 0.9838 |

Figure S7. MSD curves and diffusion coefficients of a) NO3− and b) Li+ in S-LiNO3 and C-LiNO3 GPEs.

Figure S8. RDF profiles and coordination numbers of Li+ with NO3−, PVDF, and solvent molecules in a) C-LiNO3 and b) S-LiNO3 GPEs.

Figure S9. DFT-optimized structures and binding energies of PVDF with Li⁺, NO3⁻, and LiNO3 ion pairs.

Figure S10. N 1s XPS spectra of Li anodes after 500 cycles at sputtering times of 0 and 60 s with a, b) C-LiNO3 GPE; c, d) S-LiNO3 GPE.

Figure S11. F 1s XPS spectra of Li anodes after 500 cycles at sputtering times of 0 and 60 s with a, b) C-LiNO3 GPE; c, d) S-LiNO3 GPE.

Figure S12. TOF-SIMS 2D distribution maps of lithium anode SEI after 50 cycles in S-LiNO3.

Figure S13. TOF-SIMS 3D distribution map of lithium anode SEI after 50 cycles in S-LiNO3.

Figure S14. TOF-SIMS 2D distribution map of lithium anode SEI after 50 cycles in the C-LiNO3.

Figure S15. TOF-SIMS 3D distribution map of lithium anode SEI after 50 cycles in C-LiNO3.

Figure S16. Stepwise critical current density measurements of Li‖Li symmetric cells using a) S-LiNO3 GPE and b) C-LiNO3 GPE.

Figure S17. SEM images of lithium anodes after 500 cycles with a) Bare GPE; b) S-LiNO3 GPE; c) C-LiNO3 GPE.

Table S4. Comparison of reported LiNO3 reservoir/release strategies with this work.

| Ref. | LiNO3 release strategy | Membrane/electrolyte system | Cell configuration | Representative performance |
| --- | --- | --- | --- | --- |
| [1] | Separator-stored LiNO3; slow release | LiPF6/carbonate + LiNO3 separator | Li¦¦Cu; Li-MoS3 | CE > 98%@10/20 mAh cm-2 |
| [2] | PP/LiNO3/PP sandwich; sustained NO3- release | Carbonate + bilayer PP separator | Li¦¦Cu; Li¦¦NCA | CE > 95.3%@550 cycles; NCA: 103.8 mAh g-1@500 cycles |
| [3] | LiNO3@MOF nanocapsules; continuous supply | Carbonate + MOF nanocapsules | Li¦¦LCO | LCO: 90%@240 cycles; LiNO3-saturated electrolyte failed after ~60 cycles |
| [4] | Dissociated LiNO3; fast-release PVC interlayer | LNO-PVC organogel interlayer | Li¦¦Cu; Li¦¦NCM811 pouch | CE 98.6%@300 cycles; pouch: 400 Wh kg-1, 65 cycles |
| [5] | Bilayer separator; sustainable LiNO3 release | Carbonate + bilayer separator | Li¦¦LFP | LFP: 85%@800 cycles |
| [6] | LiNO3-containing GPE; polymer-network reservoir | PVDF-HFP/POSS/LiNO3 GPE | Cu¦¦Li; Cu¦¦NMC811 anode-free | Cu¦¦Li: 250 cycles; anode-free: 31.37%@50 cycles |
| [7] | Electrospun PVDF/LiNO3 nanofibers; localized release | PP + PVDF/LiNO3 nanofiber coating | Li¦¦Li; Li¦¦NMC622; Cu¦¦NMC622 anode-free | NMC622: 83%@100 cycles; anode-free: 54%@50 cycles |
| This work | C-LiNO3: bulk GPE reservoir; S-LiNO3: surface-loaded control | PVDF-based GPE | Li¦GPE¦Cu; LFP anode-free; NCM811¦GPE¦Li; LFP¦GPE¦Li | CE 96.39%@185 cycles; LFP anode-free: 151.16 mAh g-1@115 cycles; NCM811: 154.72 mAh g-1@450 cycles; high-loading LFP: 132.81 mAh g-1@700 cycles, 88.68%; LFP: 99.01 mAh g-1@3000 cycles, 71.75% |

Reference

- Shi, Q.; Zhong, Y.; Wu, M.; et al. High-capacity rechargeable batteries based on deeply cyclable lithium metal anodes. Proc. Natl. Acad. Sci. USA 2018, 115, 5676–5680. https://doi.org/10.1073/pnas.1803634115.

- Liu, Y.; Qin, X.; Zhou, D.; et al. A biscuit-like separator enabling high performance lithium batteries by continuous and protected releasing of NO3− in carbonate electrolyte. Energy Storage Mater. 2020, 24, 229–236. https://doi.org/10.1016/j.ensm.2019.08.016.

- Liu, Q.; Xu, Y.; Wang, J.; et al. Sustained-release nanocapsules enable long-lasting stabilization of Li anode for practical Li-metal batteries. Nano-Micro Lett. 2020, 12, 176. https://doi.org/10.1007/s40820-020-00514-1.

- Stuckenberg, S.; Bela, M.M.; Lechtenfeld, C.T.; et al. Influence of LiNO3 on the Lithium Metal Deposition Behavior in Carbonate‐Based Liquid Electrolytes and on the Electrochemical Performance in Zero‐Excess Lithium Metal Batteries. Small 2024, 20, 2305203. https://doi.org/10.1002/smll.202305203.

- Li, S.; Liu, Y.; Wang, K.; et al. Sustainable release of LiNO3 in carbonate electrolytes for stable lithium metal anodes. Chem. Commun. 2024, 60, 2649–2652. https://doi.org/10.1039/d3cc05859j.

- Yim, T.; Kim, K.; Hassig, M.Q.; et al. Lithium-Nitrate-Containing Gel Polymer Electrolyte for Carbonate-Based Anode-Free Lithium Metal Batteries. ACS Appl. Mater. Interfaces 2025, 17, 37851–37862. https://doi.org/10.1021/acsami.5c03252.

- Haidar, A.H.; Hawari, N.H.; Anggreini, D.; et al. PVDF Nanofiber Separator with Sustained LiNO3 Additive Release for Dendrite-Suppressed Anode-Free Lithium Metal Batteries. J. Mater. Chem. A 2026, 14, 12449–12460. https://doi.org/10.1039/d5ta09302c.